Plastics 001		                             Name_____________________

Introduction to Plastics                               _______                                                       Date___________

Exam #1	                                         238

- Name and describe the two basic morphologies of thermoplastic materials (10 pts)

______________________________________________________________________________________

______________________________________________________________________________________

______________________________________________________________________________________

______________________________________________________________________________________

- What was the first fully synthetic plastic material, who invented it, and when was it invented? (5 pts)

______________________________________________________________________________________

______________________________________________________________________________________

- What is viscoelasticity and what causes it? (10 pts)

______________________________________________________________________________________

______________________________________________________________________________________

______________________________________________________________________________________

- Having certain atoms in the polymer chain increase the flexibility and make the material hygroscopic. What are the elements and why do they make the polymer chain more flexible? Sketch if it helps  (5 pts)

______________________________________________________________________________________

______________________________________________________________________________________

______________________________________________________________________________________

______________________________________________________________________________________

- List whether the following materials are Semi-crystalline (S) or Amorphous (A)

(+3 pt/ -10 pts each) It’s only -10 if you answer incorrectly – blanks are -5)

_____ PVC 		_____ PET	   ______ ABS   		_____PMMA		_____ Nylon 6/6 30%GF

_____  GPPS    	_____ POM 	    _____ HDPE	  	 _____ Nylon 6/6		_____ PP

- Thoroughly explain branching and how it affects a material’s ductility. (10 pts)

______________________________________________________________________________________

______________________________________________________________________________________

______________________________________________________________________________________

______________________________________________________________________________________

- Name and describe the two primary polymerization reactions. (10 pts)

______________________________________________________________________________________

______________________________________________________________________________________

______________________________________________________________________________________

______________________________________________________________________________________

- One type of reaction is more likely to have a narrow molecular weight distribution and a much lower degree of branching. Which type is it and why does it possess these qualities? (10 pts)

______________________________________________________________________________________

______________________________________________________________________________________

______________________________________________________________________________________

______________________________________________________________________________________

- Enter either an ↑, ↓, or NC (no change) for the following material properties (2 pt each)

  - An increase in temperature

____Modulus		____Impact strength 	____ Density

____ Viscosity		____Yield Strength	____ Creep			_____ Toughness

  - An increase in test speed (strain rate)

____Modulus		____Impact strength 	____ Density

____ Viscosity		____Yield Strength	XXXX Creep			_____ Toughness

  - Increasing the molecular weight

____Modulus		____Impact strength 	____ Density

____ Viscosity		____Yield Strength	____ Creep			_____ Toughness

  - A decrease in crystallinity

____Modulus		____Impact strength 	____ Density

____ Viscosity		____Yield Strength	____ Creep			_____ Toughness

- Why does Polypropylene have a higher Tg than PE? (3 pts)

______________________________________________________________________________________

______________________________________________________________________________________

______________________________________________________________________________________

______________________________________________________________________________________

- Draw and Label Polyethylene and Polystyrene (10 pts)

- Name the plastic materials that are made from the following monomers (10 pts)

______________________________		___________________________________

- What was the time period when man started modifying natural polymers?____________________________(3 pts)

- Thoroughly explain the difference between a thermosetting and a thermoplastic resin (5 pts)

______________________________________________________________________________________

______________________________________________________________________________________

______________________________________________________________________________________

______________________________________________________________________________________

- Name an instance where you would want a wider molecular weight distribution and explain why. (5 pts)

______________________________________________________________________________________

______________________________________________________________________________________

______________________________________________________________________________________

______________________________________________________________________________________

- Plastic molecules have a high aspect ratio, what does this mean? (3 pts)

______________________________________________________________________________________

______________________________________________________________________________________

- ______________________________ When small groups of monomers are attached to the main chain of another polymer (3 pts)

- ___________________________________________________When there are three types of ‘mers’ polymerized together (3 pts)

- ____________________________ When one type of ‘mer’ alternates with another mer in a chain with no specific pattern (3 pts)

- In ______________________________________, the CH3 side groups are all arranged on the same side of the main chain (3 pts)

- In _______________________________________________________, the side groups alternate with no apparent order.  (3 pts)

- In one type of polymerization reaction only a part of the molecule reacts, what is the name of that part? (3 pts)

_________________________________________________

- Explain how Orientation increases the properties in the direction of orientation, but lessens them perpendicular to the orientation (3 pts)

______________________________________________________________________________________

______________________________________________________________________________________

______________________________________________________________________________________

______________________________________________________________________________________

You have the following 3 different polymers;

Polymer A at a molecular weight of 450,000 g/mole.

Polymer B at a molecular weight of 250,000 g/mole

Polymer C at a molecular weight of 200,000 g/mole

- If you mixed 2,000 lb of polymer A with 1,000 lb of B, and 500 lb. of C, what would be:

The number of moles of Polymer A? _______________ moles (2 pts) (2 decimal places)

The number of moles of Polymer B? _______________ moles (2 pts) (2 decimal places)

The number of moles of Polymer C? _______________ moles (2 pts) (2 decimal places)

The weight fraction of Polymer A? ___________% (2 pts) (1 decimal place)

The weight fraction of Polymer B? ___________% (2 pts) (1 decimal place)

The weight fraction of Polymer C? ___________% (2 pts) (1 decimal place)

The Mw? ______________________ g/mole (5 pts) (0 decimal places)

The Mn? ______________________ g/mole (5 pts) (0 decimal places)

- You have an unlimited supply of polymers A and B.  You are trying to achieve a Mw of 400,000 g/mole. What is your mix ratio?

Ratio of A:B _____:_____ (10 pts)

Bonus: 1 pt each

Name 6 advantages and 3 disadvantages of plastic materials

Adv _______________________________________________	Dis _______________________________________

_______________________________________________	      ________________________________________

_______________________________________________    	      _________________________________________

_______________________________________________

_______________________________________________

_______________________________________________