Plastics 001	                       	                        Name______________

______________

Quiz #3	                                                             40                                                                   Date___________

You have the following 5 different polymers;

Polymer A at a molecular weight of 50,000 g/mole.

Polymer B at a molecular weight of 20,000 g/mole

Polymer C at a molecular weight of 2,000 g/mole

Polymer D at a molecular weight of 1,000 g/mole

Polymer E at a molecular weight of 500 g/mole

- If you mixed 2,000 lb of each polymer, what would be:

The number of moles of Polymer A? _______________ moles (2 pts)

The number of moles of Polymer B? _______________ moles (2 pts)

The number of moles of Polymer C? _______________ moles (2 pts)

The number of moles of Polymer D? _______________ moles (2 pts)

The number of moles of Polymer E? _______________ moles (2 pts)

The weight fraction of Polymer A? ____________% (2 pts)

The weight fraction of Polymer B? ____________% (2 pts)

The weight fraction of Polymer C? ____________% (2 pts)

The weight fraction of Polymer D? ____________% (2 pts)

The weight fraction of Polymer E? ____________% (2 pts)

The Mw? _______________ (5 pts)

The Mn? _______________ (5 pts)

- You have a material silo filled with Polymer B at 250,000 lbs. It doesn’t possess the melt strength necessary for your blow molding operation; you need some lower viscosity material added so you can lower the temperatures and make the material more like taffy and less like water. You have a large quantity of Polymer D on hand and need to mix enough in to lower the Mw by 40%.

How many lbs of Polymer D do you add? ________________________________lbs. (10 pts)