Plastics 001	                                                 	    Name______________

______________

Quiz #4                                                             65                                                                Date___________

- Name and describe the two basic morphologies of thermoplastic materials. (10 pts)

Amorphous – Random arrangement of polymer molecules

Semi-crystalline  - a portion of the molecular chain folds up into densely packed areas

- Name and describe the three (3) main types of bonds (or forces) found in organic chemistry. Put an * next to the most important type (10 pts)

*Covalent bonds – sharing of electrons

Ionic bonds – One atom takes a molecule from the other atom – charged and the charge causes attraction

Van der Waals forces – slight charge on the polymer chains causes them to be attracted to each other

- List 4 of the 5 factors that affect a materials chain flexibility and material properties. They have to do with the arrangement and effects (10 pts)

  - Temperature

  - Branching

  - Sidegroups

  - Types of Bonding

  - Additives    (bonus +2)

- What are the two main factors that affect a material’s viscoelasticity and how does each affect it? (10 pt)

  - Temperature – hotter the easier the chains can slide past each other – more free volume

  - Strain Rate – Pull slower – easier for chains to slide past one another

- What is viscoelasticity and what causes it? (10 pt)

Polymer molecules stretch and they flow

It is because of their structure – long, thin molecules – high aspect ratio

- Define Tg? (10 pt)

Glass transition temperature – temperature at which a material goes from a glassy solid to a rubbery solid

How does Tg affect each type of material morphology?

Amorphous – whole mass of material gets rubbery and more ductile

S/C – amorphous portion gets rubbery, high enough above Tg and crystals can form

- Define Tm? (10 pt)

Melt temperature – temperature at which the crystals in the material will melt

How does Tm affect each type of material morphology?

S/C – all crystals in the material melt and it flows very easily

Amorphous – don’t truly melt – temperature at which we can process the material

- List whether the following materials are Semi-crystalline (S) or Amorphous (A)

(+2 pt/ -4 pts each) It’s only -4 if you answer incorrectly – blanks are -2)

__A__  GPPS    	__a__ PVC	    __s__ HDPE	   __a___ ABS		__s___ PP

__s___ Nylon 6/6	___s__ POM	   ___s___ PET  	__a__PMMA	__s___ Nylon 6/6 30%GF