Plastics 001	                                             	    Name__Master_______________

______________

Quiz #7                               		           22                                        Date____________________

- What is the amount of material that is pumped in front of the screw during the plastification stage called? (2 pts)

____Shot Size_________________________________________________________________________________________

- During the filling stage, how full is the cavity when injection is finished?(2 pts)

___95 – 98%__________________________________________________________________________

- Why do you need the packing stage? (2 pts)

____To compensate for the polymer shrinkage when it cools___________________________________________________

- What type of gas is used in Gas-Assist? (2 pts)

___Nitrogen__________________________________________________________________________________________

- What are the two reasons you would use Gas-Assist? (2 pts)

___To add strength and reduce weight_____________________________________________________________________

- Both Gas-Assist and Structural foam use the gas to finish doing what during the filling stage? (2 pts)

___Filling the cavity____________________________________________________________________________________

- By changing the barrel temperature, you can affect what material property?  (2 pts)

___Viscosity__________________________________________________________________________________________

- Name 2 advantages of Injection Molding: (2 pt each)

  - _High Production Rates, High Tolerances, Hot Runners – Low Scrap Rate,_

  - _Minimal Labor, Complex Shapes, and Excellent Surface Finish_________

- Name 2 disadvantages of Injection Molding: (2 pt each)

  - _High Tooling Cost, Part Details not Easy to Construct, Warpage after Molding,_

  - _Long Mold Building Time, and Hard to Predict Shrinkage__________________